SPECIFICATION TEXT PROPOSAL 
Secumat® Cell 150 
		
Pos.: ……. Quantity: …..…… Unit Price: ……………. Total Price: ………………… 
Geosynthetic erosion control cell, Secumat® Cell 150 or equivalent, made by Naue GmbH & Co. KG, used as an erosion control system. Function supply and installation according to design, layout plans and manufacturer’s installation guidelines.

Secumat® Cell 150 is a three-dimensional erosion control product for permanent reduction against the consequences of erosive precipitation in round-grained or coarser soils.
The product consists of chemically and biologically resistant solid cell walls welded together for soil and root stabilisation. The cell walls have perforations so that there is a hydraulic coupling of the cells. To improve the contact to the soil, the surface of the cells is textured. Soil particles and plant roots can embed well in these cells.
The product can be used over a wide surface for erosion control. It is used to stabilise the soil surface in earthworks, landfill construction, traffic route construction and hydraulic engineering.

The geocell is permanently connected section by section with the Secumat® Screw connecting element (screw plus nut), which is included in the scope of delivery. Quantities are based on the area to be covered. Material for cut-off must be included in the calculation.

The following parameters must be considered for proof of equivalency:

Technical Data:

Raw material:			Polyethylene (PE)

Thickness of cell wall:
(according to ASTM D 5199)			1.4 mm

Cell area:			491 cm²

Cell dimensions:			34.2 cm / 28.7 cm / 15 cm

Number of perforations per cell:					4 times 12 perforations

Perforation diameter:						20 mm

Texture depth:							0.3 mm

Colour:								black

Tensile strength:
(according to EN ISO 13426-1)					22.5 kN/m

Shear strength:
(according to EN ISO 13426-1)					12.7 kN/m

Split strength:
(according to EN ISO 13426-1)					24.2 kN/m

Connection strength:
(according to ISO 101319)						19.4 kN/m

Section Dimensions:

Width x Length:							3.18 m x 10.9 m

Diameter:								15 cm

Weight:								14.3 kg

The following proofs must be submitted with the tender:

•	Certified quality management system according to DIN EN ISO 9001:2015
•	Certified environmental management system according to DIN EN ISO 14001:2015
•	The product must be covered within two weeks after installation. However, an immediate covering may be required depending on project specific conditions.

Optimal fixing:

The Secumat® Cell 150 should be permanently secured to the ground with an anchoring system in accordance with the project-specific requirements or the manufacturer´s installation guidelines. For the fixation, concrete bar steel (to be provided by the customer; e.g. B550B; 18 mm ≥ diameter ≥ 10 mm; length = 3 x cell height, unless otherwise defined for the project) and Secumat® PinCap end caps are to be used and installed according to the installation guidelines.

Proof of Delivery (POD)
Secumat® Cell 150
Naue GmbH & Co. KG
Gewerbestraße 2
32339 Espelkamp
GERMANY
Tel.: +49 57 43 41-0
Fax: +49 57 43 41-240
E-Mail: info@naue.com
www.naue.com  							Status: 03.03.2022