SPECIFICATION 
Secugrid® HS 1000/100 R6

Pos.: ……. Quantity: ….…… Unit Price: ……………. Total Price: ………………… 
  
Geogrid, Secugrid® HS 1000/100 R6 or equivalent, made by NAUE GmbH & Co. KG, used as reinforcement according to manufacturer’s installation guideline.

Secugrid® HS 1000/100 R6 is a geogrid made of high tenacity polyester (PET) filaments with an extruded polyethylene (PE) protective coating with welded junctions used for reinforcement in many fields of civil engineering, including landfill engineering, road construction and hydraulic engineering. 

The following parameters have to be considered for proof of equivalency:

Technical Data:

Raw Material:							Polyester (PET)

Nominal Tensile Strength:						≥ 1000 / ≥ 100 kN/m
(longitudinal/transverse) (DIN EN ISO 10319)

Tensile Strength at 2% Elongation:				240 kN/m
(longitudinal) (DIN EN ISO 10319)

Elongation at Nominal Tensile Strength: 			≤ 10.5 / ≤ 10.5 %
(longitudinal/transverse) (DIN EN ISO 10319)

Extensional Stiffness at 1% Strain:				17,000 kN/m
(longitudinal) (DIN EN ISO 10319)

Max. creep strain at 45 % degree of utilisation:			≤ 0.5 %
(1day-120 years, to be confirmed by isochronous curves)

UV-Resistance of protective coating:				high
(EN 12224)

Durability of protective coating:					100 years
(EN 13249:2016 ff, Annex Durability)

Long-term design strength TD:					≥ 565 kN/m
(longitudinal, 120 years, coarse gravel ≤ 35mm, 
pH 4.1-9.0; according to BBA/HAPAS Certificate)
Construction related strain:						0 %

Product Identification/Imprint:					max. 5.0 m distance

Roll Dimensions
Width x length 							4.75 m x 100 m

Quality assurance
•	Manufacturer has to be certified according to EN ISO 9001
•	Product needs to provide CE marking
•	Durability (Annex B) of min. 100 years for the use in natural soils with a pH-value between 4 and 9 and a soil temperature of <25°C.
•	Valid BBA-certificate for verification of product specific reduction factors

Proof of Delivery (POD)
Secugrid® HS 1000/100 R6
NAUE GmbH & Co. KG
Gewerbestraße 2
32339 Espelkamp-Fiestel
Germany
Tel.: +49 57 43 41 - 0
Fax: +49 57 43 41 - 240
E-Mail: info@naue.com
www.naue.com  
										Status: 09.2019