SPECIFICATION TEXT  
Secugrid® 120/40 R6 
		
Pos.: ……. Quantity: …...…… Unit Price: ……………. Total Price: ………………… 
  
Geogrid, Secugrid® 120/40 R6 or equivalent, made by Naue GmbH & Co. KG, used as reinforcement according to manufacturer’s installation guideline.

Secugrid® 120/40 R6 is a geogrid made of stretched, monolithic, textured polyester flat bars (PET) with welded junctions used for reinforcement in many fields of civil engineering, including landfill engineering, road construction and hydraulic engineering. The geogrid must not be coated with a separate polymer. Quantities are based on area to be covered. Wastage due to overlapping and cut-off must be included.

The following parameters must be considered for proof of equivalency:

Technical Data:

Raw Material:							Polyester (PET)

Nominal Tensile Strength:						≥ 120 / ≥ 40 kN/m
(md/cmd) (DIN EN ISO 10319)

Tensile Strength at 2% Elongation:				42 kN/m
(longitudinal) (DIN EN ISO 10319)

Elongation at Nominal Tensile Strength: 			≤ 7 / ≤ 7 %
(longitudinal/transverse) (DIN EN ISO 10319)

Extensional Stiffness at 1% Strain:				2,400 kN/m
(longitudinal) (DIN EN ISO 10319)

Max. creep strain at 30 % degree of utilisation:			≤ 0.50 %
(120 years, to be confirmed by isochronous curves
for a period between 1 hour – 120 years)

Long-term design strength TD:					≥ 77.0 kN/m
(longitudinal, 120 years, coarse gravel ≤35mm, pH 4.1-9.0; 
according to BBA/HAPAS Certificate)

Construction related strain:						0 %

Product Identification/Imprint:					max. 5.0 m distance

Roll Dimensions
Width x length 							4.75 m x 100 m

Quality assurance
•	Manufacturer must be certified according to EN ISO 9001
•	Product needs to have CE marking
•	Environmental-Product-Declaration
•	Durability (Annex B) of min. 100 years for the use in natural soils with a pH-value between 4 and 9 and a soil temperature of <25°C.
•	Valid BBA-certificate for verification of product specific reduction factors

Proof of Delivery (POD)
Secugrid® 120/40 R6 
Naue GmbH & Co. KG
Gewerbestr. 2
32339 Espelkamp
Germany
Tel.: +49 57 43 41 - 0
Fax: +49 57 43 41 - 240
E-Mail: info@naue.com
www.naue.com  
										Status: 08.2023